Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

REGISTER OF APPROVED ENCAPSULANT PRODUCTS PAGE 1

Encapsulants are coatings applied in liquid forms that are made to be long-lasting barriers over lead paint. Conventional paint is not an encapsulant.  Only the products listed on this Register are approved for use in Massachusetts, pursuant to the regulations for Lead Poisoning Prevention and Control, 105 CMR 460.000.  Each approved encapsulant product will bear the D/L Laboratories seal of approval. The products listed on this Register have Massachusetts approval for lead paint abatement on interior surfaces with wooden, plaster, metal or masonry substrates. Encapsulant use is prohibited on floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows for regulatory compliance.

| Product Name | Manufacturer | Not Recommend for use on: | Required Dry Film Thickness | Respiratory Protection Required | Occupancy During Application |
| --- | --- | --- | --- | --- | --- |
| L-B-C Lead Barrier Compound Type III aka Childguard® | Fiberlock Technologies Inc. 150 Dascomb Road Andover, MA 01810 (978) 623-9987 (800) 342-3755 www.fiberlock.com | - Walls with chalking or calcimine - Ceilings with calicmine - Working radiators which exceed 240oF. - Friction and Impact surfaces of doors and windows. | 7 mils minimum | For spray application, use molded polymesh shell dust and mist respirator- MSHA, NIOSH Approval No. TC21C-287 or equivalent | - Occupants must be out during the day for spray application only. - Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. - Use adequate ventilation during the first 24 hours after application. |
| Lead Block | Complementary Coatings Corp. 101 Paragon Dr., Montvale, NJ 07645 800-225-5554 | - Walls with chalking or calcimine - Door jambs - Window sills - Ceilings with calcimine - Working radiators - If not top coated with alkyd or latex enamel, handrails, railing caps, cabinets and drawers - Friction surfaces | 14 to 16 mils min. | SAME AS ABOVE | SAME AS ABOVE |
| Insl-Cap Lead Encapsulating Compound | Complementary Coatings, Corp. 101 Paragon Dr., Montvale, NJ 07645 800-225-5554 | - Walls with chalking or calcimine - Door jambs - Ceilings with calcimine - Working radiators Friction surfaces | 7 mils min. | SAME AS ABOVE | SAME AS ABOVE |
| REFERENCES: Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program Encapsulants: Guidelines for Tenants and Property Owners by Childhood Lead Poisoning Prevention Program Massachusetts General Law MGL c. 111, 189A through 199B (the Lead Law) Regulations for Lead Poisoning Prevention and Control (105 CMR 460.000) FOR MORE INFORMATION: Please call the Childhood Lead Poisoning Prevention Program at 1 (800) 532-9571 or 781-774-6611 (out of state); www.mass.gov/dph/clppp |  |  |  |  |  |

Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

REGISTER OF APPROVED ENCAPSULANT PRODUCTS PAGE 2

Encapsulants are coatings applied in liquid forms that are made to be long-lasting barriers over lead paint. Conventional paint is not an encapsulant.  Only the products listed on this Register are approved for use in Massachusetts, pursuant to the regulations for Lead Poisoning Prevention and Control, 105 CMR 460.000.  Each approved encapsulant product will bear the D/L Laboratories seal of approval. The products listed on this Register have Massachusetts approval for lead paint abatement on interior surfaces with wooden, plaster, metal or masonry substrates. Encapsulant use is prohibited on floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows for regulatory compliance.

| Product Name | Manufacturer | Not Recommend for use on: | Required Dry Film Thickness | Respiratory Protection Required | Occupancy During Application |
| --- | --- | --- | --- | --- | --- |
| LEADSTOP | Complementary Coatings Corp. 101 Paragon Dr., Montvale, NJ 07645 800-225-5554 | - Walls with chalking or calcimine - Door jambs with calcimine - Window sills - Ceilings - Working radiators - If not top coated with alkyd or latex enamel, handrails, railing caps, cabinets and drawers - Friction surfaces | 14 to 16 mils min. | SAME AS ABOVE | SAME AS ABOVE |
| L-B-C Lead Barrier Compound -Type I | Fiberlock Technologies, Inc. 150 Dascomb Road Andover, MA 01810 (978) 623-9987 (800) 342-3755 www.fiberlock.com | - Walls with chalking or calcimine - Ceilings with calicmine - Working radiators which exceed 240oF. - Friction and impact surfaces of doors and windows. | 7 mils min. | SAME AS ABOVE | SAME AS ABOVE |
| SE-110 –MS (multi-purpose primer) Penetrating- Stabilizer and SE-120 (top coat) Protective- Skin. | Contact the manufacturer regarding availability through approved distributors and contractors. SAFE Encasement Systems 4344 San Cascina St Las Vegas, NV 89145 (888) 277- 8834 www.safeencasement.com | - Walls with chalking or calcimine - Ceilings with calcimine - Friction and impact surfaces | SE-110-5 mills SE-120-7 mills min. | SAME AS ABOVE | SAME AS ABOVE |
| REFERENCES: Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program Encapsulants: Guidelines for Tenants and Property Owners by Childhood Lead Poisoning Prevention Program Massachusetts General Law MGL c. 111, 189A through 199B (the Lead Law) Regulations for Lead Poisoning Prevention and Control (105 CMR 460.000) FOR MORE INFORMATION: Please call the Childhood Lead Poisoning Prevention Program at 1 (800) 532-9571 or 781-774-6611 (out of state); www.mass.gov/dph/clppp |  |  |  |  |  |

.

Revised 6/16/2000 for SAFE Encasement Systems Revised 11/22/2010

Commonwealth of Massachusetts - Department of Public Health

Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

ENCAPSULANT PRODUCT FACT SHEET

Encapsulants are coatings applied in liquid form that are made to be long-lasting barriers over lead paint.  Conventional paint is not an encapsulant. The Regulations for lead poisoning prevention require a lead inspection and a surface assessment be performed before encapsulants are applied. The Regulations allow encapsulants to be applied by a Licensed Deleading Contractor, a homeowner or a homeowner’s agent. If a homeowner or his/her agent will be applying the encapsulant, they must first be authorized by CLPPP by reading a training booklet taking a quiz, and mailing or faxing the quiz to CLPPP (781.774. 6700). Contact CLPPP for more information at 1-800-532-9571 or

www.mass.gov/dph/clppp

The use of properly applied encapsulant products with the D/L Laboratories seal of approval can satisfy Massachusetts requirements for lead paint abatement. The product named on this Fact Sheet has Massachusetts approval for deleading.

NAME: LBC® Lead Barrier Compound Type III or Childguard®

REQUEST MSDS FROM: www.fiberlock.com

Fiberlock Technologies, Inc. 150 Dascomb Road, Andover, MA 01810

PRODUCT DESCRIPTION: DL-12362

Type:  elastomeric-thermoplastic water-based copolymer 			Mixing: ready to use, mix thoroughly

Finish: Architectural Matte Color(s): white, antique linen, black 		Dry Time: 2-4 hrs (to touch)

Tintable:  Yes - contact manufacturer   Dilutable: no 			Full Cure: 30 days

Mixable with Another Product: no Paintable: yes 			Type of Cure: coalescence

Sizes: 1, 5, 55 U.S. gallon containers 					Flash Point: none

Disposal: in accordance with local, state and federal regulations 		VOC: 88 grams per liter

Application Equipment: airless spray (best), brush, roller 			Clean-Up: warm, soapy water

Spreading Rate to Achieve Required 7 Mils Dry Film Thickness

|  | No.Coats | Thickness Per Wet Coat | Thickness Per Dry Coat | Spreading Rate Per Wet Coat |
| --- | --- | --- | --- | --- |
| Brush or Roller | 2 | 7 mils | 3 - 4 mils | 240 sq.ft./gal |
| Airless Spray | 1 | 14 mils | 7 - 8 mils | 120 sq.ft./gal |

Spreading Rate to Achieve Required Dry Film Thickness - 120 sq.ft./gal

Note:  Spreading rate does not include any loss during application process.

| RECOMMENDED USES: | USES NOT RECOMMENDED: |
| --- | --- |
| WALLS: walls, chair rails, baseboards | WALLS: walls with chalking or calcimine |
| DOORS: doors, casings | DOORS: door jambs |
| WINDOWS: sills, aprons, casings | WINDOWS: (see prohibited list) |
| CEILINGS: ceilings without calcimine | CEILINGS: ceilings with calcimine |
| STAIRS: risers, railing caps, handrails, balusters, newel posts, stringers |  |
| OTHER: curved wooden surfaces | OTHER: radiators over 180°F, friction surfaces |
| CABINETS: nonfriction surfaces | CABINETS: friction surfaces |
| DRAWERS: nonfriction surfaces | DRAWERS: friction surfaces |

PROHIBITED: floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows.

SURFACE PREPARATION:  Prior to application of LBC Lead Barrier Compound Type III/ChildGuard, inspect all surfaces to insure that they are clean, dry and free of all foreign matter including dust, rust, grease, oil, mildew, glue size, calcimine, wax, soap, loose paint, etc. Patch and repair irregularities in surfaces with prepared vinyl patch or appropriate patching compound.  Use Fiberlock Technologies, Inc. Power Block or any other stain-blocking primer for surfaces which have been water-damaged or discolored.  For high-gloss or newly painted surfaces, wet scour with a strong detergent or surface preparation treatment, using a course scouring pad to eliminate any gloss. Thoroughly remove by washing any residual scouring material, detergent or other surface preparation material, and dry completely prior to application.  Wear gloves and protective eye wear if using caustics. See manufacturers specifications for information on other surface conditions (e.g. rust, efflorescence, etc.)

ENCAPSULANT APPLICATION:  Apply with airless spray equipment for best results.  Adjust G.P.M. and P.S.I. setting and tip size according to the production and control requirements of the job and the skill of the applicator.  Smaller pumps using smaller tips at higher P.S.I. settings are better suited for jobs requiring higher accuracy and greater control.  Larger pumps using larger tips at lower P.S.I. settings produce higher production application for large, open jobs, but require a higher level of application skill.  Apply by brush or roller at 240 sq ft/gal for 7 mils (wet) and 3-4 mils (dry) per coat.  Apply liberally and uniformly with a polyester or polyester/nylon brush to woodwork and trim.  Use a wet mil gauge to control thickness (a wet mil gauge is available from the manufacturer). Multiple coats may be necessary to achieve required 7 mils dry thickness.  Allow each coat to dry before applying additional coats. Use a trim brush to achieve a smooth finish on trim work.

OCCUPANCY DURING APPLICATION: Occupancy is permitted during brush or roller application, but not in room or interior space being encapsulated. For spray application, occupancy is prohibited during the day for worksite safety reasons. Occupants may return at the end of the workday.

OCCUPANCY AFTER APPLICATION: Yes. Use adequate ventilation for first 24 hours after application.

CAUTIONS: Use with adequate ventilation.  If respiratory irritation develops, increase ventilation or wear respiratory protection.

Use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-21C-287 or equivalent - during spray application.  Avoid contact with eyes and skin.  Wash hands thoroughly with soap and water after using.  During application, wear gloves and safety glasses or goggles.

WARRANTY:  LBC Lead Barrier Compound Type III/ChildGuard has a 20-year minimum warranty with certain limitations. (See product label.)  Notify Fiberlock Technologies, Inc. within 45 days of purchase to advise of any suspected manufacturing defects.

CARE AND MAINTENANCE:  LBC Lead Barrier Compound Type III/ChildGuard will not prevent exposure to the encapsulated lead-based paint if surface is damaged, broken or abraded.  Surfaces coated with L-B-C Lead Barrier Compound Type III/ChildGuard must beinspected routinely for holes, cracks, dents, peeling surfaces, bubbles, and any other defect, including water damage.  Damaged surfaces should be repaired and re-encapsulated immediately to prevent exposure to the lead hazard.

REFERENCES:

Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program

Register of Approved Encapsulants by Childhood Lead Poisoning Prevention Program

Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program

Material Safety Data Sheet (MSDS) for LBC Lead Barrier Compound Type III/ChildGuard by Fiberlock Technologies, Inc.

LBC Lead Barrier Compoun/ChildGuard Label from Container by Fiberlock Technologies, Inc.

Massachusetts General Law (MGL) c. 111, Sect. 189A-199B (the Lead Law)  Regulations for Lead Poisoning Prevention and Control (105 CMR 460.000)

FOR MORE INFORMATION OR PROBLEM RESOLUTION, CALL OR EMAIL:

Fiberlock Technologies, Inc. at 800-342-3755 or 978.623.9987 or info@fiberlock.com

Childhood Lead Poisoning Prevention Program at 1-800-532-9571 or 781-774-6711 (out of state)

The Licensed Deleader, who applied the encapsulant. If homeowner or agent applied product, you may wish to call a Licensed Deleader for advice or assistance.

Rev 7/25/96

Revised 11/22/2010

Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

ENCAPSULANT PRODUCT FACT SHEET

Encapsulants are coatings applied in liquid form that are made to be long-lasting barriers over lead paint.  Conventional paint is not an encapsulant. The Regulations for lead poisoning prevention require a lead inspection and a surface assessment be performed before encapsulants are applied. The Regulations allow encapsulants to be applied by a Licensed Deleading Contractor, a homeowner or a homeowner’s agent. If a homeowner or his/her agent will be applying the encapsulant, they must first be authorized by CLPPP by reading a training booklet taking a quiz, and mailing or faxing the quiz to CLPPP (781.774. 6700). Contact CLPPP for more information at 1-800-532-9571 or

www.mass.gov/dph/clppp

The use of properly applied encapsulant products with the D/L Laboratories seal of approval can satisfy Massachusetts requirements for lead paint abatement. The product named on this Fact Sheet has Massachusetts approval for deleading.

NAME: Lead Block

REQUEST MSDS FROM: www.msds.com

101 Paragon Dr., Montvale, NJ 07645 / 800-225-5554

PRODUCT DESCRIPTION: DL-10019

Type:  modified acrylic elastomeric resin 				Mixing: ready to use, mix thoroughly

Finish:  eggshell 	Color(s): decorator white, colors 			Dry Time: 4 - 12 hrs (to touch)

Tintable: yes - contact manufacturer 	Dilutable: no 			Full Cure: 14 days

Mixable with Other Products: no 	Paintable: yes (with alkyd or latex enamel)   Type of Cure: coalescence/crosslinking Sizes: 1 and 5 U.S. gallon containers 					Flash Point: none

Disposal: same as latex paint (follow local ordinances)               		VOC: < 100 grams per liter

Application Equipment: airless spray (best), brush, roller 			Clean-Up: warm, soapy water

Spreading Rate to Achieve Required 14 - 16 Mils Dry Film Thickness

Premier Coatings, Inc.

|  | No.Coats | Thickness Per Wet Coat | Thickness Per Dry Coat | Spreading Rate Per Wet Coat |
| --- | --- | --- | --- | --- |
| Brush or Roller | 3 - 4 | 8 - 10 mils | 4 - 5 mils | 200 sq.ft./gal |
| Airless Spray | 2 | 14 - 16 mils | 7 - 8 mils | 100 sq.ft./gal |

Spreading Rate to Achieve Required Dry Film Thickness - 50 sq.ft./gal

Note:  Spreading rate does not include any loss during application process.

| RECOMMENDED USES: | USES NOT RECOMMENDED: |
| --- | --- |
| WALLS: walls, chair rails, baseboards | WALLS: walls with chalking or calcimine |
| DOORS: doors, casings | DOORS: door jambs |
| WINDOWS: aprons, casings | WINDOWS: (see prohibited list) |
| CEILINGS: ceilings without calcimine | CEILINGS: ceilings with calcimine |
| STAIRS: balusters, newel posts, stringers Topcoat of alkyd or latex enamel required for railing caps, handrails |  |
| OTHER: curved wooden surfaces, nonworking radiators | OTHER: working radiators, friction surfaces |
| CABINETS: nonfriction surfaces, topcoat of alkyd or latex enamel required | CABINETS: friction surfaces |
| DRAWERS: nonfriction surfaces, topcoat of alkyd or latex enamel required | DRAWERS: friction surfaces |

PROHIBITED: floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows.

SURFACE PREPARATION:  Comply fully with product specifications. All surfaces must be clean, sound, dry and free of dust, rust, grease, oil, mildew and loose particles before application. A licensed deleader must remove all flaking andpeeling paint down to a sound surface. Repair damage with a joint compound and smooth over with a damp sponge to remove excess compound and blend into surrounding wall surface.  Remove all oil, grease, wax, smoke residues and other contaminants by washing with a suitable cleaner and rinsing with clean water. Remove mildew by washing with a solution of TSP (tri-sodium phosphate) in one gallon of water and add one quart of commercial bleach. Wear gloves and protective eye wear if using bleach solutions. For high-gloss surfaces, wet scour with TSP or a strong detergent substitute and water solution using coarse steel wool to eliminate any gloss. Thoroughly remove by washing any residual scouring material, detergent or other surface preparation material, and dry completely prior to application. Although no special primers are required, there may be occasions where a primer would be beneficial in the overall performance of the coating: prime water stains with stain blocking primer; prime chalking with penetrating chalk primer; prime bare wood with an enamel undercoater; prime drywall with a quality acrylic primer and sealer.

ENCAPSULANT APPLICATION: Apply in multiple coats. Achieve total thickness of 32-36 mils (wet), but do notexceed 36 mils. Use wet mil gauge when applying product. Do not apply if ambient temperature is below 45 F. Airless spray application in two coats (each 14-16 mils) is recommended for best results, including a smoother dry film. Use .017 to .019 inch orifice and a 60 mesh screen. If applied with a brush or roller, multiple coats are required to achieve required thickness. Expect 6-8 wet mils/coat by brush and 8-12 wet mils/coat by roller. Use a polyester or polyester/nylon brush. Use a high quality tapered trim brush with a filament density to achieve a smooth finish on all trim work. Application to a large smoothor any size rough area should be performed with a quality roller cover with a 1/2 to 3/4 inch nap. Regular paint topcoats may be applied over surfaces that have been sprayed, rolled or brushed with Lead Stop

OCCUPANCY DURING APPLICATION: Occupancy is permitted during brush or roller application, but not inroom or interior area being encapsulated. For spray application, occupancy is prohibited during the day for worksite safetyreasons only. Occupants may return at the end of the workday.

OCCUPANCY AFTER APPLICATION: Yes. Use adequate ventilation for first 24 hours after application.

CAUTIONS:  Use with adequate ventilation. If respiratory irritation develops, increase ventilation or wear respiratory protection. Use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-21C-287 or equivalent - during spray application. Avoid contact with eyes and skin. Wash hands thoroughly with soap and water after using. During application wear gloves and safety goggles.

WARRANTY: Lead Block has limited product liability for 20 years. The purchaser shall notify Complementary Coatings Corp. within 30 days after any damage arising out of any defect in manufacturing.

CARE AND MAINTENANCE:  Lead Block will not protect occupants from ingestion of the encapsulated lead-basedpaint if surface is damaged, broken, or abraded. Surfaces coated with Lead Block must be inspected routinely for holes, cracks, dents, peeling surfaces, bubbles, and any other defect, including water damage. Damaged surfaces should be repaired and re-encapsulated immediately to prevent exposure to the lead hazard.

REFERENCES:

Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program

Register of Approved Encapsulants by Childhood Lead Poisoning Prevention Program

Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program

Material Safety Data Sheet (MSDS) for Lead Block by Complementary Coatings Corp

Lead Block from Container by Complementary Coatings Corp.

Massachusetts General Law (MGL) c. 111,  189A-199B (the Lead Law)

Regulations for Lead Poisoning Prevention and Control 105 CMR 460.000

FOR MORE INFORMATION OR PROBLEM RESOLUTION, CALL:

Complementary Coatings Corp. at 1-800-225-5554

Childhood Lead Poisoning Prevention Program at 1-800-532-9571 or 781-774-6711 (out of state)

The Licensed Deleader, who applied the encapsulant. If homeowner or agent applied product, you may wish to call a Licensed

Deleader for advice or assistance.

Rev 6-7/25/96, 9/29/98; Revised 11/22/2010

Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

ENCAPSULANT PRODUCT FACT SHEET

Encapsulants are coatings applied in liquid form that are made to be long-lasting barriers over lead paint.  Conventional paint is not an encapsulant. The Regulations for lead poisoning prevention require a lead inspection and a surface assessment be performed before encapsulants are applied. The Regulations allow encapsulants to be applied by a Licensed Deleading Contractor, a homeowner or a homeowner’s agent. If a homeowner or his/her agent will be applying the encapsulant, they must first be authorized by CLPPP by reading a training booklet taking a quiz, and mailing or faxing the quiz to CLPPP (781.774. 6700). Contact CLPPP for more information at 1-800-532-9571 or

www.mass.gov/dph/clppp

The use of properly applied encapsulant products with the D/L Laboratories seal of approval can satisfy Massachusetts requirements for lead paint abatement. The product named on this Fact Sheet has Massachusetts approval for deleading.

NAME: Insl-Cap Lead Encapsulating Compound

REQUEST MSDS FROM: Complementary Coatings Corp.  101 Paragon Dr., Montvale, NJ 07645 / 800-225-5554 101 Paragon Dr., Montvale, NJ 07645 / 800-225-5554

Type: elastomeric-thermoplastic water-based copolymer 			Mixing: ready to use, mix thoroughly

Finish: eggshell Colors: white 					Dry Time: 2 to 4 hrs (to touch)

Tintable: Yes, contact manufacturer 					Dilutable: no Full Cure: 12 to 24 days

Mixable with Another Product: no 					Paintable: yes Type of Cure: coalescence

Sizes: 1, 5, US gallon containers 				Flash Point: none

Disposal: in accordance with local, state and federal regulations 		VOC: 44 grams per liter

Application Equipment: airless spray (best), brush, roller 			Clean-Up: soapy water

Spreading Rate to Achieve Required 7 Mils Dry Film Thickness

|  | No.Coats | Thickness Per Wet Coat | Thickness Per Dry Coat | Spreading Rate Per Wet Coat |
| --- | --- | --- | --- | --- |
| Brush or Roller | 2 | 9 mils | 3 - 5 mils | 180 sq.ft./gal |
| Airless Spray | 1 | 18 mils | 7 mils | 90 sq.ft./gal |

Spreading Rate to Achieve Required Dry Film Thickness: 100 sq. ft/gal

Note: Spreading rate does not include any loss during application process.

RECOMMENDED USES: 						USES NOT RECOMMENDED:

WALLS: walls, chair rails, baseboards 					WALLS: walls with chalking or calcimine DOORS: doors, casings 						DOORS: door jambs

WINDOWS: sills, aprons, casings 					WINDOWS: (see prohibited list)

CEILINGS: ceilings without calcimine 					CEILINGS: ceilings with calcimine

STAIRS: risers, railing caps, handrails, balusters, newel posts, stringers

OTHER: curved wooden surfaces					OTHER: working radiators, friction surfaces CABINETS: nonfriction surfaces 					CABINETS: friction surfaces

DRAWERS: nonfriction surfaces 					DRAWERS: friction surfaces

PROHIBITED: floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows.

SURFACE PREPARATION:  Massachusetts regulations require, and the manufacturer recommends, that a surface assessment, including an inspection and adhesion test (ASTM D3359), be performed on the surface to be coated before applying Insl-Cap Apply Insl-Cap to a clean, dry surface. Surfaces to be encapsulated must be free of all blistered, peeling or loose paint.  Clean and remove grease, wax, oil, smoke residues, and other contaminants by washing with detergent and rinsing with plenty of clean water.  Prime bare metal with Insl-X Checkrust Primer for Insl-Cap. Apply Insl-X PS-8000 PrimeLock Low VOC Primer to water stains or other discolored areas.

ENCAPSULANT APPLICATION: Apply in multiple coats, if necessary, to achieve desired 7 mils dry film thickness.  Airless spray, roller or brush may be used.

OCCUPANCY DURING APPLICATION: Occupancy permitted in general area during brush or roller application, but not in interior space being encapsulated.  For spray application, occupancy is prohibited during the time of application for worksite safety reasons only.  Occupants may return when application is done.

OCCUPANCY AFTER APPLICATION: Make sure adequate ventilation is available for the first 24 hours after application.

CAUTIONS: Use with adequate ventilation.  If respiratory irritation develops, increase ventilation or wear respiratory protection. Use NIOSH approved TC-21C-287 or equivalent during spray application.  Avoid contact with eyes and skin.  Wash hands after using. Wear impervious gloves and safety goggles or glasses for maximum protection.

WARRANTY: Insl-Cap has limited product liability for 20 years.  The purchaser shall notify Complementary Coatings Corp. or distributor where purchased to advise of any suspected manufacturing defects.

CARE AND MAINTENANCE: Insl-Cap cannot prevent exposure to the encapsulated lead based paint if surface film is damaged, broken or abraded. Routine inspection for holes, cracks, dents, bubbles, peeling, or any other defect including water damage is important to maintain maximum efficiency of this coating.  Damaged surfaces should be repaired and re-encapsulated immediately.

REFERENCES:

Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program

Register of Approved Encapsulants by Childhood Lead Poisoning Prevention Program

Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program

Material Safety Data Sheet (MSDS) for Insl-Cap Lead Encapsulating Compound by Complementary Coatings Corp.

Insl-Cap Lead Encapsulating Compound Label from Container by Complementary Coatings Corp

Massachusetts General Law (MGL) c. 111, §§ 189A through 199B (the Lead Law)

Regulations for Lead Poisoning Prevention and Control 105 CMR 460.000

FOR MORE INFORMATION OR PROBLEM RESOLUTION, CALL:

• Complementary Coatings Corp at (800) 225-5554 (or contact by fax at (888) 248-2143)

• Childhood Lead Poisoning Prevention Program at (617) 753-8400 or 1 (800) 532-9571

• Licensed Deleader, if one applied encapsulant. If homeowner or agent applied product, you may wish to call a Licensed Deleader for advice or assistance

rev 7/25/96 Revised 11/22/2010

Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

ENCAPSULANT PRODUCT FACT SHEET

Encapsulants are coatings applied in liquid form that are made to be long-lasting barriers over lead paint.  Conventional paint is not an encapsulant. The Regulations for lead poisoning prevention require a lead inspection and a surface assessment be performed before encapsulants are applied. The Regulations allow encapsulants to be applied by a Licensed Deleading Contractor, a homeowner or a homeowner’s agent. If a homeowner or his/her agent will be applying the encapsulant, they must first be authorized by CLPPP by reading a training booklet taking a quiz, and mailing or faxing the quiz to CLPPP (781.774. 6700). Contact CLPPP for more information at 1-800-532-9571 or

www.mass.gov/dph/clppp

The use of properly applied encapsulant products with the D/L Laboratories seal of approval can satisfy Massachusetts requirements for lead paint abatement. The product named on this Fact Sheet has Massachusetts approval for deleading.

NAME: Lead Stop – Dumond Chemical

REQUEST MSDS FROM: www.msds.com

101 Paragon Dr., Montvale, NJ 07645 / 800-225-5554

PRODUCT DESCRIPTION: DL-10019

Type:  modified acrylic elastomeric resin 				Mixing: ready to use, mix thoroughly

Finish:  eggshell 	Color(s): decorator white, colors 			Dry Time: 4 - 12 hrs (to touch)

Tintable: yes - contact manufacturer  Dilutable: no 			Full Cure: 14 days

Mixable with Other Products: no Paintable: yes (with alkyd or latex enamel)  Type of Cure: coalescence/crosslinking

Sizes: 1 and 5 U.S. gallon containers 					Flash Point: none

Disposal: same as latex paint (follow local ordinances)              		VOC: < 100 grams per liter

Application Equipment: airless spray (best), brush, roller 			Clean-Up: warm, soapy water

Spreading Rate to Achieve Required 14 - 16 Mils Dry Film Thickness

Premier Coatings, Inc.

|  | No.Coats | Thickness Per Wet Coat | Thickness Per Dry Coat | Spreading Rate Per Wet Coat |
| --- | --- | --- | --- | --- |
| Brush or Roller | 3 - 4 | 8 - 10 mils | 4 - 5 mils | 200 sq.ft./gal |
| Airless Spray | 2 | 14 - 16 mils | 7 – 8 mils | 100 sq.ft./gal |

Note: Spreading rate does not include any loss during application process.

RECOMMENDED USES: 						USES NOT RECOMMENDED:

WALLS:  walls, chair rails, baseboards     				WALLS:  walls with chalking or calcimine DOORS:  doors, casings  						DOORS:  jambs

WINDOWS:  aprons, casings     					WINDOWS: (see prohibited list)

CEILINGS: ceilings without calcimine     				CEILINGS:  ceilings with calcimine                  STAIRS: balusters, newel posts, stringers. Topcoat of alkyd or

latex enamel required for railing caps, handrails

OTHER: curved wooden surfaces, nonworking radiators                        	OTHER: working radiators, friction surfaces CABINETS: nonfriction surfaces, topcoat of alkyd or latex enamel required     	CABINETS: friction surfaces

DRAWERS: nonfriction surfaces, topcoat of alkyd or latex enamel required  	DRAWERS: friction surfaces

PROHIBITED: floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows.

SURFACE PREPARATION:  Comply fully with product specifications. All surfaces must be clean, sound, dry and free of dust, rust, grease, oil, mildew and loose particles before application. A licensed deleader must remove all flaking and peeling paint down to a sound surface. Repair damage with a joint compound and smooth over with a damp sponge to remove excess compound and blend into surrounding wall surface.  Remove all oil, grease, wax, smoke residues and other contaminants by washing with a suitable cleaner and rinsing with clean water. Remove mildew by washing with a solution of TSP (tri-sodium phosphate) in one gallon of water and add one quart of commercial bleach. Wear gloves and protective eye wear if using bleach solutions. For high-gloss surfaces, wet scour with TSP or a strong detergent substitute and water solution using coarse steel wool to eliminate any gloss. Thoroughly remove by washing any residual scouring material, detergent or other surface preparation material, and dry completely prior to application. Although no special primers are required, there may be occasions where a primer would be beneficial in the overall performance of the coating: prime water stains with stain blocking primer; prime chalking with penetrating chalk primer; prime bare wood with an enamelundercoater; prime drywall with a quality acrylic primer and sealer.

ENCAPSULANT APPLICATION: Apply in multiple coats. Achieve total thickness of 32-36 mils (wet), but do notexceed 36 mils. Use wet mil gauge when applying product. Do not apply if ambient temperature is below 45 F. Airless spray application in two coats (each 14-16 mils) is recommended for best results, including a smoother dry film. Use .017 to .019 inch orifice and a 60 mesh screen. If applied with a brush or roller, multiple coats are required to achieve required thickness. Expect 6-8 wet mils/coat by brush and 8-12 wet mils/coat by roller. Use a polyester or polyester/nylon brush. Use a high quality tapered trim brush with a filament density to achieve a smooth finish on all trim work. Application to a large smooth or any size rough area should be performed with a quality roller cover with a 1/2 to 3/4 inch nap. Regular paint topcoats may be applied over surfaces that have been sprayed, rolled or brushed with Lead Stop

OCCUPANCY DURING APPLICATION: Occupancy is permitted during brush or roller application, but not inroom or interior area being encapsulated. For spray application, occupancy is prohibited during the day for worksite safetyreasons only. Occupants may return at the end of the workday.

OCCUPANCY AFTER APPLICATION: Yes. Use adequate ventilation for first 24 hours after application.

CAUTIONS: Use with adequate ventilation. If respiratory irritation develops, increase ventilation or wear respiratory protection. Use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-21C-287 or equivalent

-during spray application. Avoid contact with eyes and skin. Wash hands thoroughly with soap and water after using. During application wear gloves and safety goggles.

WARRANTY: Lead Stop has limited product liability for 20 years. The purchaser shall notify Dumond Chemical within 30 days after any damage arising out of any defect in manufacturing.

CARE AND MAINTENANCE:  Lead Stop will not protect occupants from ingestion of the encapsulated lead-basedpaint if surface is damaged, broken, or abraded. Surfaces coated with Lead Stop must be inspected routinely for holes, cracks, dents, peeling surfaces, bubbles, and any other defect, including water damage. Damaged surfaces should be repaired and re-encapsulated immediately to prevent exposure to the lead hazard.

REFERENCES:

Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program

Register of Approved Encapsulants by Childhood Lead Poisoning Prevention Program

Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program

Material Safety Data Sheet (MSDS) for Lead Block by Complementary Coatings Corp

Lead Stop from Container by Complementary Coatings Corp.

Massachusetts General Law (MGL) c. 111,  189A-199B (the Lead Law)

Regulations for Lead Poisoning Prevention and Control 105 CMR 460.000

FOR MORE INFORMATION OR PROBLEM RESOLUTION, CALL:

Complementary Coatings Corp. at 1-800-225-5554

Childhood Lead Poisoning Prevention Program at 1-800-532-9571 or 781-774-6711 (out of state)

The Licensed Deleader, who applied the encapsulant. If homeowner or agent applied product, you may wish to call a Licensed Deleader for advice or assistance.

Rev 6-7/25/96, 9/29/98

Revised 11/22/2010

Commonwealth of Massachusetts -Department of Public Health

Childhood Lead Poisoning Prevention Program

Donovan Health Building, 1st floor

Randolph St. Canton Ma 02021

ENCAPSULANT PRODUCT FACT SHEET

Encapsulants are coatings applied in liquid form that are made to be long-lasting barriers over lead paint.  Conventional paint is not an encapsulant. The Regulations for lead poisoning prevention require a lead inspection and a surface assessment be performed before encapsulants are applied. The Regulations allow encapsulants to be applied by a Licensed Deleading Contractor, a homeowner or a homeowner’s agent. If a homeowner or his/her agent will be applying the encapsulant, they must first be authorized by CLPPP by reading a training booklet taking a quiz, and mailing or faxing the quiz to CLPPP (781.774. 6700). Contact CLPPP for more information at 1-800-532-9571 or

www.mass.gov/dph/clppp

The use of properly applied encapsulant products with the D/L Laboratories seal of approval can satisfy Massachusetts requirements for lead paint abatement. The product named on this Fact Sheet has Massachusetts approval for deleading.

NAME: LBC Lead Barrier Type I

REQUEST MSDS FROM: www.msds.com

Fiberlock Technologies, Inc. 150 Dascomb Road, Andover, MA 01810.

PRODUCT DESCRIPTION: DL-9977

Type:  elastomeric-thermoplastic water-based copolymer Mixing: ready to use, mix thoroughly

Finish:  eggshell Color(s): antique linen Dry Time: 2-4 hrs (to touch)

Tintable:  no - contact manufacturer   Dilutable: no Full Cure: 12-24 days

Mixable with Another Product: no Paintable: yes Type of Cure: coalescence

Sizes: 1, 5, 55 U.S. gallon containers Flash Point: none

Disposal: in accordance with local, state and federal regulations VOC: 209 grams per liter

Application Equipment: airless spray (best), brush, roller Clean-Up: warm, soapy water

Spreading Rate to Achieve Required 7 Mils Dry Film Thickness

No.Coats         Thickness Per Wet Coat Thickness Per Dry Coat      Spreading Rate Per Wet Coat

Brush or Roller  2 7 - 8 mils                          3 - 4 mils                             240 sq.ft./gal

Airless Spray 1 17 mils  7 - 8 mils  120 sq.ft./gal

Spreading Rate to Achieve Required Dry Film Thickness - 120 sq.ft./gal

Note:  Spreading rate does not include any loss during application process.

RECOMMENDED USES: USES NOT RECOMMENDED:

WALLS: walls, chair rails, baseboards    WALLS: walls with chalking or calcimine

DOORS: doors, casings     DOORS: door jambs

WINDOWS: sills, aprons, casings       WINDOWS: (see prohibited list)

CEILINGS: ceilings without calcimine    CEILINGS: ceilings with calcimine

STAIRS: risers, railing caps, handrails, balusters,

newel posts, stringers OTHER: curved wooden surfaces OTHER: working radiators, friction surfaces CABINETS: nonfriction surfaces CABINETS: friction surfaces DRAWERS: nonfriction surfaces DRAWERS: friction surfaces

PROHIBITED: floors, stair treads, thresholds, any exterior surface, as well as the sashes, parting beads, window wells, and the interior/exterior or header stops of moveable windows.

SURFACE PREPARATION: Prior to application of LBC Lead Barrier Compound Type I, inspect all surfaces to insure that they are clean, dry and free of all foreign matter including dust, rust, grease, oil, mildew, glue size, calcimine, wax, soap, loose paint, etc.  Patch and repair irregularities in surfaces with prepared vinyl patch or appropriate patching compound.  Use Fiberlock Technologies, Inc. Power Block or any other stain-blocking primer for surfaces which have been water-damaged or discolored.  For high-gloss or newly painted surfaces, wet scour with a strong detergent or surface preparation treatment, using a course scouring pad to eliminate any gloss. Thoroughly remove by washing any residual scouring material, detergent or other surface preparation material, and dry completely prior to application. Wear gloves and protective eye wear if using caustics.

ENCAPSULANT APPLICATION: Apply with airless spray equipment for best results.  Adjust G.P.M. and P.S.I. setting and tip size according to the production and control requirements of the job and the skill of the applicator.  Smaller pumps using smaller tips at higher P.S.I. settings are better suited for jobs requiring higher accuracy and greater control.  Larger pumps using larger tips at lower P.S.I. settings produce higher production application for large, open jobs, but require a higher level of application skill.  Apply by brush or roller at 200 sq ft/gal for 7-8 mils (wet) and 3-4 mils (dry) per coat.  Apply liberally and uniformly with a polyester or polyester/nylon brush to woodwork and trim.  Use a wet mil gauge to control thickness. Multiple coats may be necessary to achieve required 7 mils dry thickness.  Allow each coat to dry before applying additional coats. Use a trim brush to achieve a smooth finish on trim work.

OCCUPANCY DURING APPLICATION: Occupancy is permitted during brush or roller application, but not in room or interior space being encapsulated. For spray application, occupancy is prohibited during the day for for worksite safety reasons. Occupants may return at the end of the workday.

OCCUPANCY AFTER APPLICATION: Yes. Use adequate ventilation for first 24 hours after application.

CAUTIONS:  Use with adequate ventilation.  If respiratory irritation develops, increase ventilation or wear respiratory protection. Use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-21C-287 or equivalent - during spray application.  Avoid contact with eyes and skin.  Wash hands thoroughly with soap and water after using.  During application, wear gloves and safety glasses or goggles.

WARRANTY:  LBC Lead Barrier Compound Type I has a 20-year minimum warranty with certain limitations.  (See product label.) Notify Fiberlock Technologies, Inc. within 45 days of purchase to advise of any suspected manufacturing defects.

CARE AND MAINTENANCE:  LBC Lead Barrier Compound Type I will not prevent exposure to the encapsulated lead-based paint if surface is damaged, broken or abraded.  Surfaces coated with L-B-C Lead Barrier Compound Type I must be inspected routinely for holes, cracks, dents, peeling surfaces, bubbles, and any other defect, including water damage.  Damaged surfaces should be repaired and re-encapsulated immediately to prevent exposure to the lead hazard.

REFERENCES:

Deciding Whether to Encapsulate by Childhood Lead Poisoning Prevention Program

Register of Approved Encapsulants by Childhood Lead Poisoning Prevention Program

Care and Maintenance of Encapsulants by Childhood Lead Poisoning Prevention Program

Material Safety Data Sheet (MSDS) for LBC Lead Barrier Compound Type I by Fiberlock Technologies, Inc.

LBC Lead Barrier Compound Label from Container by Fiberlock Technologies, Inc.

Massachusetts General Law (MGL) c. 111, Sect. 189A-199B (the Lead Law)

Regulations for Lead Poisoning Prevention and Control (105 CMR 460.000) FOR MORE INFORMATION OR PROBLEM RESOLUTION, CALL:

Fiberlock Technologies, Inc. at 800-342-3755 or 978.623.9987 Childhood Lead Poisoning Prevention Program at 1-800-532-9571 or 781-774-6711 (out of state) The Licensed Deleader, who applied the encapsulant. If homeowner or agent applied product, you may wish to call a Licensed Deleader for

advice or assistance.

Rev 7/25/96; Revised 11/22/2010